CONSUMER PRODUCTS

# Engineering Plastics vs. Metals: The Smart Material
Substitution Strategy Reshaping Product Design

Why the best-designed consumer products increasingly use high-performance polymers where metal used to be the default — and how to make the switch successfully.

By Joshua U. Otaigbe, PhD  |  February 17, 2026  |  6 min read

Flaney Associates  |  Materials Engineering & Innovation

# Introduction: Why Plastics Keep Winning

Pick up your smartphone. Look at a modern laptop. The best-designed consumer products have been shaped by one of manufacturing's most important trends: systematic substitution of metals with engineering-grade polymers. Not cheap commodity plastics, but high-performance materials with properties that would have seemed impossible to achieve in plastic just two decades ago.

# The Case for Engineering Plastics

Weight — typically 4–7× lighter than steel and 1.5–2× lighter than aluminium

Design freedom — injection moulding can produce geometries impossible to machine from metal in a single step

Part consolidation — multiple metal parts can often become a single plastic component

Electrical insulation — eliminates additional insulating components in electrical assemblies

Corrosion resistance — no surface treatment or coating required for most applications

Noise and vibration damping — superior vibration absorption vs metals

Cost — typically lower part cost at high production volumes

# A Guide to Key Engineering Plastics

Polycarbonate (PC) — impact resistant, optically clear, heat resistant — phone cases, eyewear lenses, LED diffusers

ABS — good impact strength, easy to process, paintable — appliance housings, toys, automotive trim

Nylon (PA6, PA66) — strong, wear resistant, good fatigue life — gears, bearings, power tool housings

POM (Acetal) — very stiff, low friction, dimensionally stable — precision gears, hinges, zippers, fasteners

PEEK — extreme temperature and chemical resistance — high-end electronics, medical devices

PC/ABS Blend — balance of PC toughness and ABS processability — laptop and phone housings, power tools

# When Metal Still Wins

Metals retain their advantage for very high sustained loads over long periods, elevated temperatures above most polymers' service range (generally >150–200°C), electrical and thermal conductivity, and the premium scratch-resistant feel consumers associate with high-end products.

"The best material is always the one that delivers the required performance at the lowest total cost. Sometimes that is plastic. Sometimes it is metal. Often, it is both."

# The Hidden Pitfalls of Material Substitution

## Creep and Relaxation

Unlike metals, plastics deform slowly under sustained loads even well below their short-term strength. A plastic bracket holding a sustained load may slowly deform over months until it fails. Designing for creep resistance requires understanding the long-term viscoelastic behaviour of the specific polymer under specific load conditions.

## Weld Line Weakness

When plastic flows around a core pin or through multiple mould gates, the flow fronts meet and create a weld line — a plane of weakness that can be 20–50 percent weaker than surrounding material. Critical load-bearing features must avoid weld lines or the mould must be engineered to place them in non-critical areas.

## Environmental Stress Cracking

Many engineering plastics are susceptible to stress cracking when exposed to certain chemicals, cleaning agents, or assembly lubricants while under stress — causing sudden brittle fracture at stress levels far below normal strength. Compatibility between the plastic and all chemicals encountered in manufacture, assembly, and use must be evaluated.

# A Framework for Successful Substitution

Based on our experience helping product companies make successful metal-to-plastic transitions, key steps include:

Detailed load analysis — peak, sustained, and fatigue loading

Environmental analysis — temperature range, chemical exposure, UV

Material screening against the full performance envelope

Design optimisation specifically for plastic processing and load paths

Prototype testing under realistic conditions

Accelerated aging to validate long-term performance

At Flaney Associates, we guide consumer product companies through every step of this process — from material screening and design review to failure analysis of field returns.

For more information or questions, please contact the author:

Joshua U. Otaigbe, PhD

Founder & Principal Consultant, Flaney Associates

Email: info@flaneyassociates.com  |  Web: flaneyassociates.com

Schedule a free consultation at flaneyassociates.com/contact

© 2026 Flaney Associates. All rights reserved. Provided for informational purposes only.